Structural  diagram of the layers

Subsrat

= glue 5(m        	   = diélectrique 8(m        	 = aluminium / copper

Preparation

1. Prepare  6 foils of Kapton reduced to 8(m       ( X 4 for 20 pieces)

Dimension of the  circuit  being prepared.

_ 5 circuits on each foil

_ fixed to a plaque of copper 300(m

Level  L1AGND

2. – Black oxidise  the  copper support plaque (substrat)

- deposit liquid glue of 5(m  on to the plaque

- the mix needed to obtain 5(m  is 1/3 glue to 2/3 acetone

- bake the plaque for 30 mins @ 125(C

- press the following structure

- Pressure 90 high and 60 low

- I coformal sheet during the first pressing ( though as the layers build up increrase layers of conformal as needed)

- Standard cycle run in the press

      - Clean the plaque using acide sulphuric to remove access glue.

      - Brush lightly the surface with (ponce)

      - Rinse and dry in oven @ 100(C

      - Laminate with photoresist when the plaque is still warm

      - Transfer image ( note : before etching one has to remember to stop etching half way  so as to not remove the alignment marks)

      - Etch and remove photoresist

      - Brush with ponce  and rinse.

NIVEAU D1

        - DEPOSIT LIQUID GLUE ON THE PLAQUE

        - BAKE FOR 30 MINS @125(C

        - BAKE A FOIL OF KAPTON WITH ONE SIDE 5 MICRONS OF COPPER  FOR 1Hr @ 80(C

        - PRESS THE COPPER KAPTON TO THE PLAQUE USING TWO CONFORMALS

        - CLEAN THE PLAQUE AFTER PRESSING WITH SULPHURIC ACID

        - BRUSH WITH WATER TO REMOVE DISSOLVED GLUE

        - DRY IN OVEN @ 125(C

        - LAMINATE,TRANSFER IMAGE, ETCH AND STRIP (remembering to protect alignment marks )

        - BRUSH WITH PONCE SOFTLY TO REMOVED ANY RESIDUE ALU FROM THE ETCHING

        - ETCH KAPTON (protect alignment marks)

        - REMOVE COPPER USING ACID CHROMIC SO AS NOT TO ETCH THE UNDERLYING ALUMINUM

NIVEAU L2AVDD

- DEPOSIT LIQUID GLUE

- DRY IN OVEN @ 120 C

- PRESS FOIL OF ALUMINIUM ON THE PLAQUE (2 CONFORMAL)

- CLEAN RESIDUE GLUE WITH SULPHURIC ACID

- PONCE SOFTLY WITH BRUSH

- RINSE UNDER WATER USING A BRUSH TO REMOVE ECCESS GLUE

- BAKE IN OVEN @ 125 C

- LAMINATE, TRANSFER IMAGE, ETCH AND STRIP ( PROTECT ALIGNMENT MARKS

- BRUSH WITH PONCE TO REMOVE REISIDUAL TRACES OF ALU.

Niveau d2 and L3Hlines

- Deposit liquid glue to the plaque

- bake in oven at 120 C

- press foil of kapton copper to the plaque

- remove glue using sulphuric acid

- rinse and brush in water

- dry in oven 100 C

- laminate, transfer image ( micro via’s) etch and strip

- remove chromium with ponce sortly

- etch kapton and glue

- metalise via’s

- clean and dry, laminate, transfer image (tracks) etch and strip

Niveau D3 and L4Vlines

- Deposit liquid glue to the plaque

- bake in oven at 120 C

- press foil of kapton copper 15 microns  to the plaque

- remove glue using sulphuric acid

- rinse and brush in water

- dry in oven 100 C

- laminate, transfer image ( micro via’s) etch and strip

- remove chromium with ponce sortly

- etch kapton and glue

- metalise via’s

- clean and dry, laminate, transfer image (tracks) etch and strip

- plate tracks with nickle gold and clean

Niveau D4

- Deposit liquid glue to the plaque

- bake in oven at 120 C

- press foil of kapton copper 5 microns  to the plaque

- remove glue using sulphuric acid

- rinse and brush in water

- dry in oven 100 C

- laminate, transfer image etch and strip

- remove chromium with ponce sortly

- etch kapton

- remove copper

Niveau L5DVDD

- Deposit liquid glue to the plaque

- bake in oven at 120 C

- press foil of Aluminium 15 microns  to the plaque (3 conformals)

- remove glue using sulphuric acid

- rinse and brush in water

- dry in oven 100 C

- laminate, transfer image etch and strip( protect alignment marks)

- remove residual traces of aluminium with ponce softly

Niveau D5

- Deposit liquid glue to the plaque

- bake in oven at 120 C

- press foil of kapton copper 5 microns  to the plaque

- remove glue using sulphuric acid

- rinse and brush in water

- dry in oven 100 C

- laminate, transfer image etch and strip

- remove chromium with ponce sortly

- etch kapton

- remove copper

Niveau L6DGND

- Deposit liquid glue to the plaque

- bake in oven at 120 C

- press foil of Aluminium 15 microns  to the plaque (3 conformals)

- remove glue using sulphuric acid

- rinse and brush in water

- dry in oven 100 C

- laminate, transfer image etch and strip( protect alignment marks)

- remove residual traces of aluminium with ponce softly

Niveau D6 and L7FASTOR

- Deposit liquid glue to the plaque

- bake in oven at 120 C

- press foil of kapton copper 15 microns  to the plaque

- remove glue using sulphuric acid

- rinse and brush in water

- dry in oven 100 C

- laminate, transfer image etch and strip

- remove chromium with ponce sortly

- etch kapton

- clean and dry, laminate, transfer image (tracks) etch and strip

- plate tracks with nickle gold and clean

# Text boxes

Copper 5 microns

L1AGND

D1

L2AVDD

D2

L3HLINES

D3

L4VLINES

D4

L5DVDD

D5

L6DGND

D6

L7FASTOR

Kapton 8 microns

350mm

160mm

Substrat

50(m  Alu

Glue 5(m

Copper 300(m

SUBSTRAT

KAPTON 8 MICRONS

ALU 50 MICRONS

GLUE 5 MICRONS

GLUE 5 MICRONS

ALU 50 MICRONS

KAPTON 8 MICRONS

SUBSTRAT

ALU 30 MICRONS

ALU 30 MICRONS

GLUE 5 MICRONS

ALU 50 MICRONS

KAPTON 8 MICRONS

SUBSTRAT

Microvia ‘s

Cu  5 micron’s

tracks

tracks

Cu  5 micron’s

Microvia ‘s

ALU 30 MICRONS

GLUE 5 MICRONS

ALU 50 MICRONS

KAPTON 8 MICRONS

SUBSTRAT

Cu 15 micron’s

Ni Au plating

Ni Au plating

Cu 15 micron’s

tracks

Cu  5 micron’s

Microvia ‘s

ALU 30 MICRONS

GLUE 5 MICRONS

ALU 50 MICRONS

KAPTON 8 MICRONS

SUBSTRAT

Kapton 8 microns

Kapton 8 microns

Ni Au plating

Cu 15 micron’s

tracks

Cu  5 micron’s

Microvia ‘s

ALU 30 MICRONS

GLUE 5 MICRONS

ALU 50 MICRONS

KAPTON 8 MICRONS

SUBSTRAT

Aluminium 15 micron’s

Aluminium 15 micron’s

Kapton 8 microns

Ni Au plating

Cu 15 micron’s

tracks

Cu  5 micron’s

Microvia ‘s

ALU 30 MICRONS

GLUE 5 MICRONS

ALU 50 MICRONS

KAPTON 8 MICRONS

SUBSTRAT

Kapton 8 micron’s

Kapton 8 micron’s

Aluminium 15 micron’s

Kapton 8 microns

Ni Au plating

Cu 15 micron’s

tracks

Cu  5 micron’s

Microvia ‘s

ALU 30 MICRONS

GLUE 5 MICRONS

ALU 50 MICRONS

KAPTON 8 MICRONS

SUBSTRAT

Aluminium 50 micron’s

Aluminium 50 micron’s

Kapton 8 micron’s

Aluminium 15 micron’s

Kapton 8 microns

Ni Au plating

Cu 15 micron’s

tracks

Cu  5 micron’s

Microvia ‘s

ALU 30 MICRONS

GLUE 5 MICRONS

ALU 50 MICRONS

KAPTON 8 MICRONS

SUBSTRAT

Kapton copper 15 microns, imaged etched and plated in nickle gold